## Slide 1: Penetration Resolution in Computer Modeled Fabrics
Collin Blake
Contractor
AFRL/RXCC
Dr. John Whitcomb 1, Dr. Craig Przybyla 2
1. Texas A&M University 2. Air Force Research Lab

## Slide 2: Outline
Background
  Textile Simulation
Problem
Initial ideas
  Issues Encountered
Current Resolution
  Issues Encountered
  Current Issues
Future Plans

## Slide 3: Background
Evolution of composite materials lead into computational analysis and design of fiber-reinforced structures
Current focus of these materials is understanding and simulating damage initiation and propagation
Extensive research at microstructure level
Mesoscale next level

## Slide 4: Background
Evolving modelling techniques and computational ability allow us to model increasingly complex geometries for computer analysis
Modelling discrete fibers very computationally expensive
Using Homogenized Tows with matrix surrounding tows

## Slide 5: Textile Simulation
Digital chain method to generate realistic woven geometry
Discrete fiber filaments can then be converted into homogenized tows and modelled in a matrix
Creates realistic woven geometries that can be analyzed

## Slide 6: Penetration
Created geometries come with penetrating surfaces
  Tows in close proximity develop surface penetrations after tow surface creation
  Detecting Penetrations secondary problem
Conventional FEA programs cannot run analysis

## Slide 7: Initial Idea
In order to impose surface to surface contact, a plane is placed between the penetrating surfaces.
The penetrating nodes are then moved to this surface
This will ideally create a perfect contact surface between the tows

## Slide 8: Issues Encountered
Creates “Spurs” near penetration boundary
Does not account for large curvatures
Can create too large of surface, significantly altering tow topography
Matrix pockets can also occur

## Slide 9: Next Ideas
Use NURBS Surface to define penetrating surfaces
  Gives analytical solution
  Defines Penetration surface boundary
  Reduces tow volumes during fitting
  Can be difficult to redefine tow mesh along boundary
Polyhedron Penetration Detection
  Used in video game physics
  Difficult to determine penetration distance
  Used primarily as avoidance, not resolution (time dependent
Least Square Bivariate Cubic Fit Surface
  Difficult to implement
  Better fitted surface of actual tow geometry

## Slide 10: Current Solution
Find nearest neighbor of penetrating node on tow being penetrated
Compute half distance and move both nodes to location
Resolves compatibility

## Slide 11: Current Solution (cont’d)

## Slide 12: Current Solution (Cont’d)
Known Issues
  Degenerate Elements
  Nodes allowed to move outside tow boundary
  Jagged topography between tows
Possible Solutions
  Mesh cleaning to renumber elements and nodes
  Improve penetration routines
  Correct with smoothening

## Slide 13: Future Work
Work on establishing a surface between tows for better surface matching for 3-D wovens
Correct meshes to work more readily with FEA software
Evaluate reduction in tow volumes after surfaces
Work towards a Parallelization of VTMS

## Slide 14
Questions?